## Slide 1: MPM Simulations of the Mechanical Properties of Oriented Strand Board (OSB) Accounting for Undulating Strands and Imperfect Glue Bonds
Edward A. Le
Ph.D. Candidate
WS/MS Dual Major
Advisor: Prof. & Richardson Chair, John A. Nairn
5th MPM Workshop
Thursday and Friday, April 2-3, 2009 Oregon State University Corvallis, OR, 97331

## Slide 2: Overview
Introduction
  OSB manufacturing process
  Motivation
  Objectives
  Failure mechanics
Calculation of interfacial stiffness
Numerical simulation
  MPM
  Results
Conclusions
Future Plan

## Slide 3: Introduction - OSB
Source: Prof. F. Kamke
Hybrid Poplar : clone of Populus deltoides and Populus trichocarpa.
Notes: <number>
Hybrid Poplar : clone of Populus deltoides and Populus trichocarpa.
Originally envisioned as an energy crop during petroleum crisis of the 1970s
DOE provided much of the early research on genetics and silicultural activities
First commercialized by the pulp and paper industry in the early to mid-1980s as opportunity to moderate the fluctuations in fiber pricing

## Slide 4: Introduction - Motivation
OSB producers want to minimize the resin content of their board while maintaining required properties
  How much resin on each strand?
  What’s the effect of resin coverage on mechanical properties?
Can we make use of Viscoelastic Thermal Compression (VTC) strand?
  Densified strands from hybrid poplar to get stiffer and stronger material
Notes: <number>
VTC: Densification using dynamic heat, steam, and mechanical compression
Hybrid Poplar : clone of Populus deltoides and Populus trichocarpa.
Originally envisioned as an energy crop during petroleum crisis of the 1970s
DOE provided much of the early research on genetics and silicultural activities
First commercialized by the pulp and paper industry in the early to mid-1980s as opportunity to moderate the fluctuations in fiber pricing

## Slide 5: Introduction – Objectives
Study the glue-bond interfacial stiffness as a function of adhesive coverage on strands
Develop a numerical model for studying the mechanical properties of OSB as a function of glue-bond stiffness (and more)

## Slide 6: Rationale: Bondline - Fluorescence Microscopy
Source: C. Frihart 2005
Notes: <number>
Fig. 1, fluorescence microscopy is used to distinguish the adhesive from the wood. The striking
feature in this photograph is how large the wood interphase region is compared with the
interface, adhesive interphase, and bulk adhesive regions. Pictured is a relatively thick adhesive
layer; often there may be no significant bulk adhesive layer. Although interface properties are
important, this figure shows that adhesive penetration into the wood could play a dominant role.
Flow of the adhesive to fill the surface micro-roughness is important for all bonding, but
adhesive penetration into the substrate is not a significant issue in most bonding applications.
FRIHART ON BONDED WOOD PRODUCTS 3
However, good penetration into the wood is a very important aspect of wood bonding. Standards
such as ASTM D 2559 require bond formation within the minimum and maximum of the
recommended open and closed assembly times [9]. Sufficient penetration into the wood is
considered important for good bond formation, but overpenetration produces a starved bondline
that is the weak link. Overpenetration does not occur with non-porous substrates; thus, different
factors need to be considered in formulating and using wood adhesives. A lower viscosity
adhesive is normally better for the wetting and adhesion, but for wood the adhesive can be so
thin as to overpenetrate into the wood.
FIG.

## Slide 7: Glue Line Mechanics
“Perfect Interface”
Dt=
Real
Model
“Imperfect Interface”
Dt
[ut]
0
Dt
0
0
(debonded)
(where is shear stress)
Measure Dt
Goal
Adapted from Nairn, 2007
Dt is glue-line property
“Slippage”

## Slide 8: Calculation of Interfacial Stiffness Dt
FP
(1-F)P
L
G1
G2
E2
E1
L2
L1
l
t2
t3
t1
G3
E3
P
, k = specimen stiffness
C3=compliance found by Shear-Lag analysis (verified as accurate by FEA)
C3 (E1, E2, E3, t1, t2, t3, Dt)
Solve numerically for Dt given
Notes: <number>
Interfacial stiffness (MPa/mm) is extracted from Shear-lag theory of DLS specimen with an imperfect interface. Let K be measured stiffness of specimen (N/mm)

## Slide 9: Interfacial Slippage
Over 1000 tensile tests
Over 700 individual specimens of normal and VTC
Over 230 DLS specimens were prepared and tested

## Slide 10: Wood Hardening Law
Where is plastic strain
n determines the curvature
K determine the volume of the plastic strain
Notes: core

## Slide 11: Sample Simulation: OSB Compaction
40% control surface VTC
40% VTC surface strands
Core are always control strands
Notes: No interface

## Slide 12: Mechanical Testing
Load in Tension
Cantilever Beam
Bending Test
Notes: <number>
For 50% densify thickness decrease by factor of 2 then density is increase by factor of 2

## Slide 13: Simulation Results
MOE increased 10% from 1% to 25% coverage
MOE increased 23% from 1% to 100% coverage
MOE increased 12% from 25% to 100% coverage
MOE increased 56% compare to no VTC at 1/Dt=0
Notes: <number>
Adhesive (4840-4440)/4440=10% increase in MOE from 1% to 25%
(5440-4440)/4440= 23% increase in MOE form 1% to 25%
=(5440-4840)/4840=12% increase in MOE from 25% to 100%
Control (6549-4175)/4175 =56%increased

## Slide 14
Simulation Results
MOE increased 3% from 1% to 25% coverage
MOE increased 6% from 1% to 100% coverage
MOE increased 3% from 25% to 100% coverage
MOE increased 45% compare to no VTC at 1/Dt=0
Notes: Top curve (VTC)
Adhesive (3240-3140)/3140=3% increase in MOE from 1% to 25%
(3340-3140)/3140= 6% increase in MOE form 1% to 100%
(3340-3240)/3240=3%increase in MOE from 25% to 100%
Bottom curve (control)
Adhesive (1940-1740)/1740=11% increase in MOE from 1% to 25%
(2040-1740)/1740= 17% increase in MOE form 1% to 100%
(2040-1940)/1740=5% increase in MOE from 25% to 100%
(3391-2335)/2335=45% Increased

## Slide 15: Results and Discussion
All VTC on the face
  Different structure, more compaction
Notes: No interface

## Slide 16
Simulation Results: No VTC
MOE increased 7% from 1% to 25% coverage
MOE increased 18% form 1% to 100% coverage
MOE increased 10% from 25% to 100% coverage
Notes: Adhesive (3900-3650)/3650=6.85% increase in MOE from 1% to 25%
(4300-3650)/3650= 17.81% increase in MOE form 1% to 100%
(4300-3900)/3900= 10.26% increase in MOE from 25% to 100%

## Slide 17
MOE increased 10% from 1% to 25% coverage
MOE increased 29% form 1% to 100% coverage
MOE increased 15% from 25% to 100% coverage
MOE increased 70%, 80%, 95% and 116% compare to no VTC
Simulation Results: Surface VTC Strands
Notes: Adhesive (6800-6200)/6200=9.68% increase in MOE from 1% to 25%
(7800-6200)/6200= 28.8% increase in MOE form 1% to 100%
(7800-6800)/6800= 14.7% increase in MOE from 25% to 100%
=(8000-3700)/3700=116% Increased in MOE compare to no VTC at 1/Dt=0
=(4400-2600)/2600=69.23% Increased in MOE compare to no VTC at 1% coverage
=(5200-2900)/2900=79.3% Increased in MOE compare to no VTC at 25% coverage
=(6400-3300)/3300=94.94% Increased in MOE compare to no VTC at 25% coverage
10% increased in MOE from 1% to 25% coverage
29% increased in MOE form 1% to 100% coverage
15% increased in MOE from 25% to 100% coverage
70%, 80%, 95% and 116% increased in MOE compare to no VTC at 1%, 25%, 100% and at perfect interface

## Slide 18
Homogenized R-O-M
t=Thickness, E = Modulus
=Fraction of strand material
Ignores undulations, cannot model interface
C=Fraction compacted
t1 E1
t2 E2
t1 E1
Notes: Phi: Fraction of strand material =L/(L+G)

## Slide 19
Simulation Results: No VTC
Notes: Adhesive (2800-2100)/2100 =33.3% increase in MOE from 1% to 25%
(3100-2100)/2100 = 47.6% increase in MOE form 1% to 100%
(2140-1940)/1940 = 10.3% increase in MOE from 25% to 100%

## Slide 20
Simulation Results: Surface VTC Strands
Notes: Adhesive (6600-5200)/5200=26.92% increase in MOE from 1% to 25%
(7600-5200)/5200= 46.15% increase in MOE form 1% to 100%
(7600-6600)/6600= 15% increase in MOE from 25% to 100%
(11857-5855)/5855=100.2% Increased in MOE compare to no VTC

## Slide 21: Experiment: Density Profile
No VTC
Courtesy of Vardam Rathi
1.08g/cm3
0.600g/cm3
0.820g/cm3

## Slide 22: Simulation: Density Profile
No VTC

## Slide 23: Experiment: Density Profile
40% by weight VTC surface strands
Courtesy of Vardam Rathi
0.97g/cm3
0.96g/cm3
0.48g/cm3

## Slide 24: Simulation: Density Profile
40% by weight VTC surface strands

## Slide 25: Conclusions
Interfacial stiffness can be measured with DLS specimen and varies significantly from 1% to 100%
Simulations show that adhesive coverage on strands affects MOE of OSB panels
MPM is useful tool for modeling mechanical properties of wood based composites
More work is needed to determine Dt more precisely

## Slide 26: Future Plans
Continuing investigation the effect of interfacial properties of adhesives on mechanical behavior of OSB panels.
Investigating the effect of moisture content on mechanical properties of OSB.
Studying the effect of bending properties of OSB using MPM for different amounts of compaction.
Further investigation of MPM on elastic and plastic behavior to simulate OSB compaction/tension load.
Study the effect of the gap size and strand length.

## Slide 27: Acknowledgements
Prof. John Nairn for financial support and guidance
Prof. Fred Kamke for supplied the PF resin and hybrid poplar strands and experimental input
Prof. Greg Smith for uniformly dispersed resin onto wood strands
Ph.D. Committee
Dr. Peter Kitin for SEM
WSE dept. staff, Milo, Connie, Camille
Research Group (Noah, Ariji, Dr. L. Xue)
Graduate Student (Guenter, Varda, Ning, Kai, Farzana, Xiaoou, Debbie, David)