## Slide 1: Alternative Aspects of Cohesive Crack Modeling With MPM
Jason Sanchez
University of New Mexico
5th MPM Workshop
April 2009

## Slide 2: Fracture Energy: Ideal Case
Fracture Energy = Gf is amount of energy dissipated per unit crack area formed.
key material property in discrete constitutive models of fracture (Hillerborg et al. 1976)
Idealized measurement of fracture over an isolated representative volume of inhomogeneous material (concrete)




L

## Slide 3: Motivation: Size Effect in Fracture Energy Measurements
Measured by work of fracture method
Size effect observed in measured mode I Gf for concrete (Whittmann et al., 1990) – complete development of fracture process zone is inhibited by boundaries
P
P
Compact Tension Sample (CTS)
dominant crack
b

## Slide 4: Research Objectives
Simulate measured size effect Gf using a modified multiple smeared crack model (MSCM) in MPM
Evaluate performance of smeared crack model in MPM
  Stress locking (observed in smeared crack analysis in FEM)
  Mesh orientation bias of results (observed in smeared crack analysis in FEM)
Hypothesis - allowing simultaneous development of multiple cracks over a representative volume and removing energy availability restrictions for failure will reflect a size effect with constant Gf*

## Slide 5: Discrete Constitutive Models of Fracture
stress and failure plane orientation predicted by de-cohesion function
crack surface
representative material volume
traction separation law
Specific discrete model is for geological materials (Schreyer, 2007)
traction separation law built into de-cohesion function
Mode I fracture of interest: Rankine model

## Slide 6: Multiple Smeared Crack Model (MSCM)
Smeared crack idealization of cracks
in a representative volume
=
+
+
=
+
+
Actual cracks
in a representative volume
Classical MSCM (Rots, 1988)
Modified MSCM
Only one crack can develop at time
Multiple cracks allowed to develop at once
Energy availability for failure
Energy availability for failure

## Slide 7: CTS Simulation Dimensions & Properties
b = 15, 30, 60 cm (ligament length)
d = 12 cm (depth)
 – dominant crack tip position (initiation of de-cohesion)
values taken from Whittmann et al., 1990
P
P
b / 2
b
b
h
d
2.4 b


dominant crack
dominant crack tip

## Slide 8: Material Point Method (MPM)
2-D explicit MPM (Sulsky et al. 1994, 1995, 1996, 2004)
4 material points per element
velocity boundary condition applied
notch width is length of one element
de-cohesion confined to notch line
notch line

## Slide 9: 2 Cases Analyzed
CASE 1 (ideal fracture case)
  2 failure planes allowed
  predetermined orientations
CASE 2
  number of failure planes not restricted
  failure plane orientations not specified

## Slide 10: Load vs. Displacement: Cases 1 & 2
Case 1
Case 2

## Slide 11: Energy Absorbed During Fracture

## Slide 12: Results
b (cm) | Ef / (bd) (N/m) | Efd / (bd) (N/m) | % Ef from dominant crack | % Ef from non-dominant cracks
15 | 147 | 120 | 82 | 18
30 | 165 | 114 | 69 | 31
60 | 178 | 103 | 58 | 42
no size effect for case 1
size effect for case 2

## Slide 13: Conclusions & Future Work
Use of modified MSCM results in a simulated size effect trend (preliminary work)
Validation with fracture energy size effect data
  effect of shape of softening function
  implicit calculation of Gf*?
Evaluate performance of smeared crack model in MPM
  stress locking, mesh orientation bias of results, smearing over grid element vs. material point
  used in more complex problems like sea ice dynamics (Sulsky et al. 2007)

## Slide 14: References
D. Sulsky, S. Zhou, and H.L. Schreyer (1995) , Application of a particle-in-cell method to solid mechanics, Comput. Phys. 87 236-252
D. Sulsky and H.L. Schreyer (2004) , MPM simulation of dynamic material failure with a decohesion constitutive model, European Journal of Mechanics A/Solids. 23 423-445
D. Sulsky, Z. Chen, and H.L. Schreyer (1994) , A particle method for history-dependent materials, Comput. Methods Appl. Mech.. 118 179-196.
D. Sulsky and H. L. Schreyer, Axisymmetric Form of the Material Point Method with Applications to Upsetting and Taylor Impact Problems, Comput. Meths. Appld. Mechs. Engrg., 139 (1996) 409-429.
F.H. Whittmann, H. Mihashi, and N. Nomura (1990) , Size effect on fracture energy of concrete, Engineering Fracture Mechanics, 35 107-115.
A. Hillerborg, M. Modeer, and P.E. Petersson (1976) , Analysis of crack formation and crack growth in concrete by means of fracture mechanics and finite elements, Cement and Concrete Research. 6 773-782.
Rots, J.G. (1988), Smeared Computational modeling of concrete fracture, Dissertation, Delft University of Technology, Delft, The Netherlands
H.L. Schreyer (2007) . Modeling surface orientation and stress at failure of concrete and geological materials, Journal For Numerical And Analytical Methods In Geomechanics. 31 144-171.
H.L. Schreyer, D.L. Sulsky, L.B. Munday, M.D. Coon, and R. Kwok (2006), Elastic-Decohesive constitutive model for sea ice, J. Geophys. Res. 111
D.L. Sulsky, H.L. Schreyer, K.Peterson, M.D. Coon, and R. Kwok (2007), Using the material-point method to model sea ice dynamics, J. Geophys. Res. 112