## Slide 1
Jeff Burghardt
Rebecca Brannon
Jim Guilkey
Brian Leavy
Use of MPM for simulating penetration of geologic materials with particulated metal jets
University of Utah

## Slide 2: Overview
Problem description
Why MPM/GIMP?
Initial simulations
Kayenta material model
Prescribing Homogeneous Deformations in MPM
Future work/conclusions

## Slide 3: Problem description
Notes: <number>

## Slide 4: Problem description
Notes: A shaped charge is an explosive device that creates a high-velocity, high-pressure metal jet. In the petroleum industry the liner is typically composed of un-sintered metal particles. Several changes are placed in a gun body inside of a well-bore.
<number>

## Slide 5: Objectives
Predict density distribution in conical liner
Predict depth of penetration
Predict damage to target and resulting permeability
Improve upon existing methods/knowledge

## Slide 6: Importance of Spatial Variability of Material Properties
Notes: These simulations a of a tungsten sphere impacting a ceramic cylinder. The top row are the results of a finite-element simulation with three levels of mesh refinement. Failed material has been hidden from view for clarity. The solution clearly depends heavily on the mesh refinement, and does not seem to be converging. The bottom row are the results of the same simulation except that spatial variability of the yield strength has been included. The element strengths are set using a Weibull distribution and size scaling so that smaller elements are stronger than larger elements. Even at t relatively coarse mesh refinement the solution is remarkably close to the experimental result. This has dramatically mitigated mesh dependence, and increased predictiveness.
<number>

## Slide 7: Problems with Lagrangian FEM
Notes: The simulation on the left uses MPM to model penetration of a ceramic plate with copper. The simulation on the right is the same problem, only using a Lagrangian FEM scheme. After a small amount of deformation the Lagrangian FEM simulation fails due to excessive mesh distortion and entanglement. For the simulation to continue the model would have to be remeshed, which would lead to the same issues as Eularian advection.
<number>

## Slide 8: Eularian Advection Problems
Initial Strength Distribution
After Rigid Translation
Notes: The figure on the left shows the initial spatial variability of strength at the beginning of an Eularian FEM simulation. After a simple rigid translation of a few cell widths, nearly all of the spatial variability has been lost. Under a rigid translation there should have been no change in the field, but the Eularian advection scheme as spuriously smeared the field in the direction of motion.
<number>

## Slide 9: Eularian Advection Problems
Notes: This is another example of how Eularian advection eliminates any spatial variability of internal state variables with a simple rigid body translation.
<number>

## Slide 10: Why MPM/GIMP?
Advantages of MPM/GIMP:
ISV are tracked on the particles, which eliminates advection issues.
Equations of motion are solved using an Eularian description, which eliminates element distortion problems
Disadvantages of MPM/GIMP:
Momentum equations are solved somewhat less accurately than FEM
Additional computational expense as compared to FEM

## Slide 11: Overview of Plasticity Theory
Yield function determines if loading is elastic or plastic:
Elastic response:
Elastic/Plastic response:
Notes: In one dimension yield occurs when the axial stress reaches a critical value “k”. Deformation is elastic when the axial stress is smaller than k. Mathematically, we could define f= sigma – k. Then deformation is elastic if f <0, and the onset of yield corresponds to f=0. For general loading, where stress is a second-order tensor, the yield function f takes the entire stress tensor as an argument. In general, the yield function depends on the current stress state (sigma), as well as a set of internal state variables which account for loading history (here denoted collectively by the variable eta). If the yield function evaluates to a negative number, the material response is elastic and is in general governed by a nonlinear form of Hooke’s law. The fourth-order tensor relating the strain rate (epsilon dot) to the stress rate (sigma dot) is called the elastic tangent stiffness tensor. If applying elasticity theory would result in the yield function being greater than zero, the material response is elastic-plastic. A different set of equations governs elastic-plastic response. During plastic loading, the yield function is required to remain equal to zero. The fourth-order tensor relating the strain rate to the stress rate for elastic-plastic loading is called the plastic tangent stiffness tensor.
<number>

## Slide 12: Overview of Plasticity Theory
Stress and strain tensors are symmetric, and thus have 6 independent components:
In general, a second order tensor has nine independent components:
Notes: In general, a second-order tensor has nine independent components. Most of the second-order tensors of interest in solid mechanics, such as the Cauchy stress tensor, and logarithmic strain tensor are symmetric. This symmetry reduces the number of independent components from nine to six.
<number>

## Slide 13: Overview of Plasticity Theory
When expressed in the principal basis, there are only three nonzero components:
Which may be thought of as a point in a three-dimensional space:
Notes: To visualize stress states, the stress tensor is commonly expressed in its principal basis so that there are only three independent components. Using this representation, a stress state may be thought of as a point in “principal stress space”. Since the yield function plays such an important role in plasticity theory, it would be helpful have some way to visualize it. The set of all stress states for which the yield function evaluates to zero may be plotted as an iso-surface in principal stress space. This surface is often referred to as the yield surface. Points on the interior of the yield surface represent elastic states.
<number>

## Slide 14: Overview of Plasticity Theory
Commonly used yield surfaces
Notes: These are some commonly used yield surfaces. Because isotropic yield functions depend only on principal stresses and because the yield function values should be unchanged when the ordering of the principal stresses are changed, any isotropic yield function has a degree of symmetry about the [111] hydrostat. Specifically, any cross-section perpendicular to the hydrostat has six-fold symmetry.
<number>

## Slide 15: Load Path Characterization
Purpose:
Validation using simpler, well characterized material
Characterize the nature of the loading during penetration events
Direct constitutive model calibration experiments.
Direct constitutive model development.
Identify possible issues with MPM/GIMP.
Aluminum Target
Particulated Metal Jet
Notes: A set of simulations were performed using an aluminum target and a particulated metal jet. The purpose of these tests is to determine the nature of the loading in stress space. Knowledge of the nature of the loading in stress space will indicate what types of loading are likely to occur, and help to direct constitutive model development toward those loading regimes.
<number>

## Slide 16: Load Path Characterization
Lode coordinates are a more convenient alternative to traditional coordinate systems:
TXE (θ=30º)
Shear (θ=0º)
TXC (θ= -30º)
Shear (θ=0º)
θ
Shear (θ=0º)
TXC (θ= -30º)
Shear (θ=0º)
TXE (θ=30º)
Shear (θ=0º)
Shear (θ=0º)
TXC (θ= -30º)
Notes: Rather than using the three principal stresses as coordinates for visualization, it is often convenient to use so-called Lode coordinates. These coordinates represent a cylindrical coordinate system with the z-axis lying along the hydrostat ([111] axis). The z coordinate sigma_z is a measure of pressure or hydrostatic stress. The radial coordinate sigma_r is equal to the magnitude of the stress deviator, and is thus a measure of shear stress. The angular coordinate theta provides information about the ordering of the principle stresses. A Lode angle of zero indicates a state of pure shear. A Lode angle of -30 degrees is a state of triaxial compression, which means that the stress state is axisymmetric with the lateral stresses being less compressive than the axial stress. A Lode angle of 30 degrees represents a state of triaxial extension, which is a axisymmetric state of stress with the lateral stresses being more compressive than the axial stress. With these coordinates, any stress state can be uniquely specified by the r, z, and theta invariants.
<number>

## Slide 17: Z-Invariant (Pressure)

## Slide 18: R-Invariant (shear)
Notes: <number>

## Slide 19: Lode Angle
(TXC)
(TXE)
(Shear)

## Slide 20: Kayenta Constitutive Model
Notes: The yield surface used in Kayenta. Important features are:
Yield surface cap to allows for pore collapse
Greater strength in TXC than TCE, the ratio of which may vary with pressure
<number>

## Slide 21: Kayenta Constitutive Model
Supports nonlinear kinematic and/or isotropic hardening
Supports material softening and damage
Parameters may be selected to mimic simpler models (Drucker-Prager, Von-Mises, Linear Elasticity…)
Extensively verified

## Slide 22: Homogeneous Deformation in MPM
Equivalent to single-element test in FEM
Arbitrarily specified homogeneous deformations/rotations required to extensively verify constitutive models.

## Slide 23: Prescribed Deformation in MPM
Notes: Motion can be described by defining a function which describes the current position (x) of a material point in terms of the initial position of a material point (X). This mapping function may be represented as a second-order tensor called the deformation gradient (F). In general the deformation gradient will be different for each material point. If the deformation gradient is the same for all material points, the deformation is said to be homogeneous. We are interested in prescribing a homogeneous deformation.

## Slide 24: Prescribed Deformations in MPM
Solve equations of motion and update grid velocities
Modifications Required for Typical MPM Code:
Interpolate grid velocities to the particles.
Modification: Overwrite grid velocity with prescribed velocity.
…
…
…
…

## Slide 25: Prescribed Deformations in MPM
Equations of motion are still satisfied:
Since deformation is homogeneous, the stress field is constant.
The prescribed deformation is equivalent to prescribing a body force equal to the acceleration resulting from the prescribed motion.

## Slide 26: Prescribed Deformation in MPM

## Slide 27: Prescribed Deformations in MPM

## Slide 28: Example Prescribed Deformation

## Slide 29: Kayenta Benchmark Test

## Slide 30: Future Work/Conclusions
Compare aluminum target simulations to experimental data
Perform meso-scale characterization simulations
Further verify installation of Kayenta

## Slide 31: Questions?